## Slide 1: Concrete Flatwork Construction
Sidewalks
Exterior Slabs on Grade
Concrete Pavement
Presented by: Jim Tofte with Rob Murray
Facilities Engineering Architectural Civil Section

## Slide 2: Concrete Principles
  Strong in Compression/Weak Tensile Strength
  Water/Cement Ratio - Strength - Mixture - Admixtures - Curing
  Strength & Durability (Air Entrainment – Freeze/Thaw)
  Thickness Slump/Air/Compressive Strength
  Most Site Pavements are Not Reinforced
    5” Sidewalks –regular traffic (pickup trucks, passenger vehicles) 6”
    8” - trucks and buses, Major Interstates 10”-12”
    Placed on Compacted Subgrade
    Crack Control for Shrinkage (WWF or Fibers)
    Load Transfer Dowels
  Structural Slabs – Reinforced
    (loading docks, crane pads, dumpster pads, poor soils, fire lanes, bridging)

## Slide 3: Pre-Placement Meeting
ATTENDEES:
  Lead Finisher, Contractor Foreman, PM
  FE SME/Maintenance Program Mgr.
  Design Engineer Rep., FE or Consultant
  Owner/Facility Rep.
  Supplier
  Testing Lab, in an Ideal World
  Others

## Slide 4: Labor
  Union Labor Required for work with concrete materials
    Complex! Can Require Official Interpretations.
      FCS Contracts, CU Labor Relations
      BTC Representative
  Qualifications
    Ideal is ACI Flatwork Certification in CU Standards
      Exam & 1,500 hour for ACI certification
    Contractors Flatwork Concrete Resume is the norm.

## Slide 5: Submittals and Inspections
  Submittals
    Mix Design (Severe Exposure)
      5,000 psi, W/C Ratio 0.40
      Aggregates
      Admixtures
      Compare with Batch Ticket
    Crack Control: WWF or Fibers
    Reinforcing
  Testing Lab
    Open Line of Communication
    Required Information to Testing Agency
    Special Inspections
      Form work
      Rebar
      Subgrade
      Concrete Testing
      Concrete Sampling (Cylinders)

## Slide 6: Pre-Placement Materials On Hand
  Finishing Tools/Methods
    Correct edgers, finishing tools, Concrete Saws
    Surface Finish, Broom Type, etc.
  Curing Materials
    Curing Materials
    Water On Site/Available Water, Hoses, Sprayers, etc.
    Blankets (if approved)
    Intermediate Curing Compound
    Spray Cure & Seal (if approved)
    High / Low Thermometers
  Protection
    Poly Sheeting (Rain)
    Temperature
    Signage and Barricades

## Slide 7: Finishing
  Type (broomed, smooth, etc.)
    What type of broom finish, rough, smooth, direction.
  Joints (Location, Spacing, Layout)
    Control (Sawcut is standard), City Standard (Tooled)
    Expansion Joints
      Fiber Board
      Dowels
  Mockups?
  Embedded Objects (anchor bolts, ADA Tiles, etc.)

## Slide 8: Weather/Mitigation
  Forecasted Weather
  Extreme Heat Low Humidity
    Size of finishing crew (sets up faster)
    Intermediate curing, fog or mist spray
    Retarders
  Cold Weather Concrete
    Special Section in Specifications
    Heated Mix
    Heated subgrade
    Tenting
    Heat/Blankets
  Rain
    Poly sheeting
    Is runoff directed away from placement?
RM

## Slide 9: Curing & Protection
  Curing
    Wet Curing 7 Days (uninterrupted)
    Non-Contact Curing is standard in most areas
    Maintain Temperature during curing
    Liquid Cure and Seal (Egress/Code, Approvals needed)
    Cure and Seal Products (ACI C309)
    Protection
      Sealer, Penetrating Salt Inhibitor
        Types
      Barricades, Signage, etc.
    Caulking Joints
    Temperatures
    Protection of Caulk
    Remove Caps and Application

## Slide 10: Building Project Success
RM

## Slide 11: What keeps us up at night !
    Neighbors Dog!
    Poor Communication!
    Curing Supplies not on site!
    Not enough hoses, water source not available!
    Not getting cure on same day! It is possible !
    Letting pour dry out so you can saw cut it! What?
    Proper curing “not always” a priority for contractors, so it seems.
    We have Improved! Kudos!
    “Cost of Propper Curing is in our Bids, lets make sure it is getting done!”

## Slide 12: Engage Facilities Engineering (FE):
    FE is here to Help. Campus Stewardship.
    Engage FE early in the design process.
    Encourage consultants to reach out to FE with any questions regarding our Design and Construction Standards.
    Please invite us to pre-placement meetings.
    Consider engaging FE more actively in your project.
    (Great examples: Statler, NCRE, West Ave, Feeney Way)
  FE - Architectural and Civil Section:
  Flatwork Concrete/ Sidewalks / Pavements
  Jim Tofte jt743@cornell.edu
  Structural Engineering / Bridges / Building Systems
  Rob Murray rmb234@cornell.edu